LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion®						          Predispersed Rubber Chemicals

CBS-80       Accelerators for the Vulcanization of Natural and Diene Synthetic Rubbers

Product description

| Composition | 80% N-cyclohexyl-2-benzothiazyl sulphenamide based on specification, 20% EPDM binder and dispersing agents |
| --- | --- |
| Appearance | Grey granules |
| Density,20 oC | Approx. ~ 1.19 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of CBS: Melting point; ~ 96 oC; Evaporation loss; ≤ 0.5 %. CBS content; ≥ 94 %; Insoluble in ethanol; ≤ 0.4 %. Ash content; ≤ 0.4 %; Sieve residue 63µm; ≤ 0.1 %. Free amine; ≤ 1.0 %. |

Use Characteristics		The curing accelerator HiDispersion® CBS-80 provides a considerably long scorch time, great processing safety and a fast full cure. HiDispersion® CBS-80 is used as a sole accelerator for the low sulphur vulcanization or in combination with dithiocarbamate or thiuram accelerators. The vulcanizates obtained have good ageing resistance and a good compression set. The scorch time of compounds containing HiDispersion® CBS-80 in combination with thiurams and dithiocarbamates is noticeably reduced. Thiourea has a strong secondary acceleration effect on HiDispersion® CBS-80, mainly in mixes containing little sulphur. In compounds which are accelerated with mercaptanes and thiu-rams, HiDispersion® CBS-80 may delay scorch

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easy quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective CBS is assured.

Dosage levels	NR:	primary:  0.5 – 1.0 phr with 2.5 – 3.5 phr sulphur

secondary:  0.5 phr with 1.5-3.0 phr sulphur and 0.3 phr mercapto or thiuram accelerators

SBR: 1.0 – 1.4 phr with 1.5 – 2.5 phr sulphur and 0 – 0.2 phr thiuram accelerator

Applications	Automotive and construction profile, Tire treads, air hoses, conveyor belts, footwear and other technical articles.

Packing			Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.