LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion®						          Predispersed Rubber Chemicals

CTP-80       Retarder Agents for the Vulcanization of Natural and Diene Synthetic Rubbers

Product description

| Composition | 80% N-(cyclohexylthio) phthalimide, 20% EPDM binder and dispersing agents |
| --- | --- |
| Appearance | Beige granules |
| Density,20 oC | Approx. ~ 1.23 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of CTP: Melting point; ~ 90 oC; Evaporation loss; ≤ 0.5 %. CBS content; ≥ 96%; Sieve residue 63µm; ≤ 0.1 %. Ash content; ≤ 0.4 %. |

Use Characteristics		The curing retarder HiDispersion® CTP-80 retards the onset of cure in NR and diene sythetic rubbr without considerably extending the total curing time. It is preferably used with sulphenamide or thiazole accelerators to improve processing safety, keeping the properties of the vulcanizate unchanged. HiDispersion® CTP-80 significantly improves the storage stability of uncured diene rubber compounds. When HiDispersion® CTP-80 is used in the compounds, it is possible to process the rubber compounds at higher temperatures, thereby ensuring full use of machine capacity. Contact staining does not occur. HiDispersion® CTP-80 causes only very slight discolouration in bright or white articles.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective CTP is assured.

Dosage levels	Normally 0.2 - 2.0 phr

Applications	Compounds based on synthetic diene rubber and natural rubber, which are mainly cured with  thiazole and sulphenamide accelerators (e.g. in the production of tires, conveyor belts, soles, technical moulded and extruded articles).

Packing			Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.