LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Additives)

HiDispersion®						          Predispersed Rubber Desiccants

CaO-80      Desiccant for rubber compounds of extrusion processing to prevent porosity

Product description

| Composition | 80% Finely selected calcium oxide, 20% EPDM binder and dispersing agents |
| --- | --- |
| Appearance | Grey granules |
| Density,20 oC | Approx. ~ 2.25g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |

Use Characteristics		HiDispersion® CaO-80 is a desiccant provided in EPDM rubber predispersed granules. Normal CaO binds the moisture by the formation of calcium hydroxide (Ca(HO)2). The enables the  production of vulcanizates to be cured without pressure and which, otherwise,  even in using vacuum extruders, show porosity due to the moisture still present in the compounds. This is why HiDispersion® CaO-80 is preferably used in extrusion compounds which have to be cured continuously either in open hot air, fluid beds, salt baths or in the UHF equipment. HiDispersion® CaO-80 and also be recommended for the use in expanded compounds, particularly in microcellular sponge, because HiDispersion® CaO-80 provides a more uniform cell structure.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective CaO is assured.

Dosage levels	The normal dosage is between 2 and 10 phr. It is mainly determined by the expected moisture content which mostly depends on the amount and type of filler used.

Applications	Automotive and construction profile sealants, belts, straps, conveyor belts, rollers, cable coverings, rubber floorings.

Packing			Net 20 kg cartons containing individually vacuum packed aluminum-bags of 2 kg.

Storage stability	In original closed containers under cool and dry conditions max. 12 months.

Handling	Consult material safety data sheet (MSDS) for additional handling information.