LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion®						          Predispersed Rubber Chemicals

DOTG-70       Accelerator for the vucalnization of NR and synthetic rubbers

Product description

| Composition | 70% N,N'-di-o-tolyl guanidine, 30% EPDM binder and dispersing agents |
| --- | --- |
| Appearance | Dark grey granules |
| Density,20 oC | Approx. ~ 1.10 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of DETU: Melting point; ~ 171 oC; Evaporation loss; ≤ 0.5 %. CBS content; ≥ 96%; Sieve residue 63µm; ≤ 0.5 %. Ash content; ≤ 0.5%. |

Use Characteristics		The accelerator HiDispersion® DOTG-70 causes very slow onset of cure and a relatively slow rate of cure. HiDispersion DOTG-70, used on its own, causes a strong rever- sion; therefore the use of effective antioxidants is recommended.

When HiDispersion DOTG-70 is used in combination with mercapto, sulphenamide, thiuram and dithiocarbamate accelerators, reciprocal activation and secondary acceleration can be achieved. The crosslinking density and rate of cure are increased. Good mechanical properties and good ageing resistance are obtained. HiDispersion DOTG-70 has no tendency to bloom in the vulcanizates.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective DOTG is assured.

Dosage levels	In NR	primary: 0.8 - 1.2 phr DOTG-70 with 2.5 - 4 phr S-80;

secondary: 0.05-0.4 phr DOTG-70 with 1-1.5 phr MBTS-80 and 1.5-3 phr S-80;

In SBR	0.1 - 0.4 phr DOTG-70 with 1 - 1.5 phr MBTS-80 and 1.5 - 2.5 phr S-80;

In NBR	0.05 - 0.4 phr DOTG-70 with 1.5 - 2.4 phr S-80 and 0.8 - 1.5 phr CBS-80.

Applications	Technical articles (especially thick-walled ones), band tires, roller coverings, cable compounds.

Packing			Net 25kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.