LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion®						          Predispersed Rubber Chemicals

DPG-80       Accelerators for the Vulcanization of Natural and Diene Synthetic Rubbers

Product description

| Composition | 80% N,N'-diphenyl guanidine based on specification, 20% EPDM binder and dispersing agents |
| --- | --- |
| Appearance | Grey granules |
| Density,20 oC | Approx. ~ 1.14 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of DPG: Melting point; ~ 144 oC; Evaporation loss; ≤ 0.3 %. DPG content; ≥ 96 %; Sieve residue 63µm; ≤ 0.1 %. Ash content; ≤ 0.4 %. |

Use Characteristics		The curing accelerator HiDispersion® DPG-80 gives a very long scorch time and a relatively slow full cure. It causes slight discolouration and cannot be used in light-coloured articles, except as an activator. When HiDispersion® DPG-80 is used on its own the resistance of the vulcanizates to hot air and oxygen is poor (requiring the use of effective antioxidants). Accelerators of the mercapto type are strongly activates by HiDispersion® DPG-80. In IIR and EPDM compounds, HiDispersion® DPG-80 has only little effect.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easy quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective CBS is assured.

Dosage levels	primary: 1 - 2 phr with 2,5 - 3,5 phr sulphur;

secondary: 0,1 - 0,25 phr with 0,75 - 1 phr mercapto accelerator and 2,5 phr sulphur.

Applications	Automotive and construction profile, Tire treads, air hoses, conveyor belts, footwear and other technical articles.

Packing			Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.