LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion®						          Predispersed Rubber Chemicals

DPTT-70   Ultra accelerator for the vulcanization of natural and diene synthetic rubbers, respecially curing agent for sulfurless or low sulfur vulcanization.

Product description

| Composition | 70% dipentamethylene thiuram tetrasulphide, 30% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | Beige granules |
| Density,20 oC | Approx. ~ 1.25 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of DPTT: Melting point; ~ 105 oC; Evaporation loss; ≤ 0.3 %. DPTT content; ≥ 96 %; Sieve residue 63µm; ≤ 0.5 %. Ash content; ≤ 0.5 %. |

Use Characteristics		The curing accelerator HiDispersion® DPTT-70 causes a very rapid and scorch-safe vulcanization of natural and sythetic rubbers. In combination with mercapto and sulphenamide accelerators, HiDispersion® DPTT-70 is used as an activator and secon- dary accelerator.

HiDispersion® DPTT-70 is also used, in small amounts, in combination with other thiuram accelerators. The vulcanizates are then characterized by exceptionally good resistance to ageing. HiDispersion® DPTT-70 is normally used for NR, SBR, NBR, IIR, BR, Hypalon etc.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion during the rubber mixing. Therefore, optimal activity of the effective DPTT is assured

Dosage levels	0.35 - 3.5 phr for heat aging resistance rubber articles of all kinds.

Applications	It can be used as sulfurless curing agent, and it produces heat aging resistance rubber articles of all kinds, e.g. hoses, seals, bushing, especially based on EPDM and IIR. When used with MBTS-80, it can be used as accelerator for Hypalon rubber.

Packing			Net 25 kg cartons with plastic inner。

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.