LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion®						          Predispersed Rubber Chemicals

DTDM-80   Ultra accelerator for the vulcanization of natural and diene synthetic rubbers, respecially curing agent for sulfurless or low sulfur vulcanization.

Product description

| Composition | 80% morpholine disulfide (4,4'-dithiodimorpholine), 20% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | White to beige granules |
| Density,20 oC | Approx. ~ 1.25 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of DTDM: Melting point; ~ 118 oC; Evaporation loss; ≤ 0.5 %. DTDM content; ≥ 96 %; Sieve residue 63µm; ≤ 0.8 %. Ash content; ≤ 0.5 %. Sulfur content; 25.0-29.0%. |

Use Characteristics		The curing accelerator HiDispersion® DTDM-80 liberates free sulphur which, in contrast to normal sulphur, mainly forms mono and diether bridges under normal curing conditions. These are responsible for excellent heat ageing resistance of the vulcanizates. HiDispersion® DTDM-80 causes no blooming effects which are generally observed when using thiuramdisulphides as crosslinking agents. In contrast to compounds with HiDispersion® CLD-80, compounds with HiDispersion® DTDM-80 stand out for their increased safety in scorch properties. When the full curing temperature is reached, a quick vulcanization follows. Acid compounding ingredients may cause a premature decomposition of HiDispersion® DTDM-80 and thus reduce the excellent scorch safety (long scorch time). In general the use of HiDispersion® DTDM-80 is recommended whenever favourable compression set behaviour and advantageous ageing behaviour is required.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective DTDM is assured.

Dosage levels	NR and SBR							with carbon black				light color fillers

HiDispersion® DTDM-80			1.0  - 2.0					1.0 - 2.0	phr

HiDispersion® S-80				0.25 - 1.0					0 .25 - 1.0 phr

HiDispersion® CBS-80				0.5 - 0.75						-	phr

HiDispersion®  MBTS-80				-						0.3 - 0.5	phr

HiDispersion®  TMTD-80				-						0.3 - 0.5	phr

NBR and IIR							NBR						IIR

HiDispersion® DTDM-80			1.0 - 2.0						1.2 - 2.0	phr

HiDispersion® S-80				0.0 - 0.5                      1.0 - 1.75	phr

HiDispersion® CBS-80				1.5 - 3.0							-	phr

HiDispersion® MBTS-80				-						1.0 - 2.5	phr

HiDispersion® TMTD-80			0.5 - 2.5						1.0 - 2.5	phr

For sulfurless vulcanization

HiDispersion® DTDM-80			1.25 - 2.0 phr

HiDispersion® CBS-80				1.0   - 1.5 phr

HiDispersion® TMTD-80			1.0   - 1.5 phr.

Applications	articles resistant to reversion based on NR, such as tyre carcasses and  age-resistant articles based on SBR, NBR and EPDM.

Packing			Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.