LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Chemicals)

HiDispersion						          Predispersed Rubber Chemicals

IS 60-80           Curing agent for all natural and diene synthetic rubbers

Product description

| Composition | 80% Total sulfur (60% insoluble and 40% soluble sulphur) 20% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | Yellow granules |
| Density,20 oC | Approx. ~ 1.61 g/cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |

Use Characteristics		HiDispersion IS 60-80 contains 80 % of total sulphur type, which is 60 % insoluble in carbon disulphide and other solvents as well as 40 % of soluble sulphur.  HiDispersion IS 60-80 is a vulcanizing agent for all natural and synthetic rubber compounds in which sulphur bloom or infiltration of neighbouring layers of compound should be avoided. The use of insoluble sulphur HiDispersion IS 60-80 is therefore to be recommended for all applications that require no blooming, mutilayer curing, or where good ply-adhesion is essential.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective total sulfur is assured.

Dosage levels	Same phr with normal powder IS 60, normally 1-5phr.

Applications		All types of tires, conveyor belts, retreading tire, assembled hoses,  technical articles, e.g. seals, rollers etc

Packaging	Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.