LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Antioxidants)

HiDispersion 						          Predispersed Rubber Chemicals

MB-80       Non-staining antioxidant for vulcanizates based on natural and synthetic rubbers

Product description

| Composition | 80%2-mercaptobenzimidazole 20% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | White-grey granules |
| Density,20 oC | Approx. ~ 1.27 g/cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of MBT: Melting point; ~ 290 oC; Evaporation loss; ≤ 0.5 %. MBT content; ≥ 98%. Ash content; ≤ 0.5 %. |

Use Characteristics		HiDispersion MB-80 is a non-staining antioxidant for light-coloured and white rubber compounds. It is used as a synergist for other antioxidants. The effect of the combination of HiDispersion MB-80 with other antioxidants is greater than the sum of the effects of the individual components. The combination of HiDispersion MB-80 with antiozonant IPPD is suitable for extremely heat resistant vulcanizates. It also provides the vulcanizates with some protection against copper and manganese poisoning. The efficiency of HiDispersion MB-80, used on its own, depends to a large extent on the curing system. HiDispersion MB-80 gives better results in combination with dithiocarbamate and thiuram accelerators than in combination with other accelerators.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective MB is assured.

Dosage levels	As antioxidant: 0.6 - 1.5 phr

As antioxidant, specially for steam-resistant grades: 2.0 - 3.0 phr

for transparent grades: 0.4 phr.

Applications	Rubber articles which must withstand oxygen, heat and steam; heat-resistant rubber articles which are produced by thiuram vulcanization; white, coloured and transparent articles of all kinds; fabric proofings.

Packing			Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.