LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion 						          Predispersed Rubber Chemicals

MBTS-75   Semi-ultra accelerator for the vulcanization of natural and diene synthetic rubbers

Product description

| Composition | 75% dibenzothiazyl disulphide 25% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | Beige granules |
| Density,20 oC | Approx. ~ 1.32 g/cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of MBTS: Melting point; ~ 165 oC; Evaporation loss; ≤ 0.5 %. MBTS content; ≥ 98%; Sieve residue 63µm; ≤ 0.5 %. Ash content; ≤ 0.4 %; Free MBT; ≤ 0.8 %. |

Use Characteristics		HiDispersion MBTS-75 is very popular used for NR, SBR, NBR, CR, and BR, although it is similar to MBT-80, tendency to cause weak scorch, and have a longer induction period for curing. It can be used independently or together with basic accelerator in the same way as MBT-80. It can also be used together with TMTD-80. HiDispersion MBTS-75 is a versatile semi-super accelerator with good processing safety. In combination with activated dithiocarbamtes, HiDispersion MBTS-75 prevents scorching. It is activated by thiurams, dithiocarbamates and aldehyde-amines. During the processing and vulcanization of CR compounds it has a retarding effect. When used with ultra-accelerators, HiDispersion MBTS-75 improves the processing safety. Vulcanizates produced with HiDispersion MBTS-75 show good ageing properties.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective MBTS is assured.

Dosage levels	NR:	primary: 1.2 – 2.2 phr with 2 - 3 phr sulfur

secondary: 0.6 – 1.2 phr with 1- 2 phr sulfur and 0.2 - 0.5 phr dithiocarbamate accelerators;

SBR: primary: 1.1 – 3.3phr with 1 - 3 phr sulfur

secondary: 0.3 - 0.8 phr with 1 - 3phr sulfur and 0.3 - 0.6 phr sulphenamide accelerators;

NBR: primary: 1.2 – 2.2 phr with 0,2 - 2 phr sulfur

secondary: 0.8 phr with 0.2 - 2 phr sulfur and 0.3 phr sulphenamide;

IIR:	0.3 – 1.2 phr with 1 - 2 phr sulfur.

Applications	Mechanical articles of all kinds, e.g. treads, carcasses, air hoses, conveyor belts, transmission belts, hoses, cable insulations.

Packing			Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.