LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion						          Predispersed Rubber Chemicals

NOBS-80     Aaccelerator for the vulcanization of natural and diene synthetic rubbers

Product description

| Composition | 80% dibenzothiazyl disulphide 20% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | Off-white to beige granules |
| Density,20 oC | Approx. ~ 1.26 g/cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of TBBS: Melting point; ~ 78 oC; Evaporation loss; ≤ 0.5 %. TBBS content; ≥ 95%; Free amine; ≤ 0.5 %. Ash content; ≤ 0.5 %. |

Use Characteristics	The curing accelerator HiDispersion NOBS-80 causes a considerably long scorch time, great processing safety and a fast full cure. HiDispersion NOBS -80 is used as primary accelerator for the low sulphur vulcanization or in combination with dithiocarbamate and thiuram accelerators. The vulcanizates obtained provide good ageing resistance and compression set. The scorch times of mixes containing HiDispersion NOBS -80 in combination with thiuram and dithiocarbamate accelerators are noticeably reduced.

Combinations of HiDispersion NOBS -80 and HiDispersion TMTM-80 have proved particulary favourable. They cause very short total curing times - though the mixes have good scorch resistance and a very high degree of crosslinking, even in relatively small amounts. Thiourea derivatives have strong secondary acceleration effects on HiDispersion NOBS -80, especially in mixes containing small amounts of sulphur. In mixes that are accelerated with mercaptanes and thiurams, HiDispersion NOBS -80 may reduce the onset of cure.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective NOBS is assured.

Dosage levels	NR: primary: 0.8 - 1.2 phr with 2.5 - 4 phr sulphur

secondary: 0.05 - 0.4 phr with 1-1.5 phr mercapto accelerator and 1.5-3 phr sulphur;

SBR: 0.1 - 0.4 phr with 1 - 1.5 phr mercapto accelerator and 1.5 - 2.5 phr sulphur;

NBR: 0.05 - 0.4 phr with 1.5 - 2.4 phr sulphur and 0.8 - 1.5 phr sulphenamide accelerator.

Applications		Tire treads, carcasses, conveyor belts, floor coverings, footwear, cable insulations.

Packing			Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.