LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion      					          Predispersed Rubber Chemicals

ZDTP-50         No-staining accelerator for fast curing of natural and diene synthetic rubbers

Product description

| Composition | 50% Zinc dialkyldithiophosphate 50% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | Semi - transparent to white granules |
| Density,20 oC | Approx. ~ 1.20 g/cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |

Use Characteristics		HiDispersion ZDTP-50 is used as a special accelerator for EPDM compounds containing accelerators of the thiazol and thiuram class as well as sulphur and zinc oxide. HiDispersion ZDTP-50causes a high degree of cross-linking. Vulcanizates  accelerated by HiDispersion ZDTP-50 show no signs of blooming when observing the  recommendation for the maximium dosage. With the use of HiDispersion ZDTP-50 accelerator systems can be obtained that exhibit a very good processing safety and storage stability of the accelerated raw compounds.  As an ingredient of EV systems HiDispersion ZDTP-50 can be used to accelerate the vulcanzation of NR, IR, SBR, NBR, IIR etc. The vulcanizates are then characterized by exceptionally good resistance to heat. HiDispersion ZDTP-50 is used as a secondary accelerator in the sulphur vulcanization of EPDM and NR in combination with sulphen amides, thiazoles and thiurams. It does not build secondary amines during the vulcanization process which can form hazardous N-nitrosamines.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective liquid ZDTP is assured.

Dosage levels	NR: ZDTP-50:2.0-3.4 phr, TMTM-80:0.3-0.6 phr, MBTS-80:0.6-0.9 phr, S-80:0.3-0.6 phr

EPDM:ZDTP-50:2.0-3.4 phr, TMTD-80:0.3-1.0 phr,MBT-80:0.6-1.9 phr, S-80:1.2-3.2 phr

Nitrosamine free EPDM:ZDTP-50 :2.0-3.4 phr, TBzTD-80:0.3-1.0 phr,MBT-80加1.2-1.9 phr, S-80:1.2-2.2 phr

Applications Technical moulded and extruded articles of all kinds, e.g. sheets, buffers, dock fenders, profiles

Packaging		Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.