LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion®						          Predispersed Rubber Chemicals

MBT-80   Semi-ultra accelerator for the vulcanization of natural and diene synthetic rubbers

Product description

| Composition | 80% 2-mercapto-benzthiazol, 20% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | Light yellow granules |
| Density,20 oC | Approx. ~ 1.33 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of MBT: Melting point; ~ 172 oC; Evaporation loss; ≤ 0.5 %. MBT content; ≥ 98%; Sieve residue 63µm; ≤ 0.5 %. Ash content; ≤ 0.5 %. |

Use Characteristics		An accelerator HiDispersion® MBT-80 which is most frequently used for NR, SBR, IIR, and CR. It is used independently or together with basic accelerators. HiDispersion® MBT-80 is a semi-ultra, multi-purpose accelerator with a long plateau effect. It provides vulcanizates with good physical properties. In sulfur-free compounds HiDispersion® MBT-80 acts as an anti-scorch agent, in CR compounds as a retarder. HiDispersion® MBT-80 is activated by basic accelerators as aldehyde amine and guanidine etc., and by thiurams and dithiocarbamates.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective MBT is assured.

Dosage levels	NR and SBR:	primary: 1 - 2 phr with 2 – 3 phr HiDispersion® S-80

secondary: 0.5 – 1 phr with 0.2 - 0.3 phr HiDispersion® TMTD-80 and 1.5 phr S

sulfurless: 0.5 phr with 3 - 4 phr HiDispersion® TMTD-80

IIR:  0.5 - 1 phr with 0.5 - 1.5 phr HiDispersion® TMTD-80  and 1 - 2 phr sulfur.

Applications	Mechanical articles of all kinds, e.g. treads, carcasses, air hoses, conveyor belts, driving belts, hoses, cable insulations.

Packing			Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.