LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Chemicals)

HiDispersion®						          Predispersed Rubber Chemicals

R-80           Used in direct bonding compounds,e.g. for resorcinol-formaldehyde-silica system

Product description

| Composition | 80% Resorcinol, 20% SBR binder and dispersing agents |
| --- | --- |
| Appearance | White to red-brown granules |
| Density,20 oC | Approx. ~ 1.20 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |

Use Characteristics		HiDispersion® R-80 is a component of the bonding system resorcinol-formaldehyde- silica. In conjunction with a formaldehyde donor (e.g. HEXA-80 or HMMM-65) the resorcinol- formaldehyde- resin, responsible for the bonding of rubber to textile and steel cords, is formed during the curing process. This system is suitable for bonding all types of rubber to reinforcing materials, e.g. fabrics, glass fibres and metals (e.g. steel-cords).

.

Processing Advantages	The predispersion of Resorcinol in a SBR binder allows quick absorption and excellent dispersion in the rubber. In this way, optimal activity of Resorcinol is assured.

Dosage levels	3 - 4 phr

Applications	Tires, conveyor belts, V-belts, round belts, fire hoses, other reinforced  hoses, flexible containers, fabric proofings.

Packaging		Net 20 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.