LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Chemicals)

HiDispersion®						          Predispersed Rubber Chemicals

S-80           Curing agent for all natural and diene synthetic rubbers

Product description

| Composition | 80% Sulfur, 20% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | Yellow granules |
| Density,20 oC | Approx. ~ 1.65 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of Sulfur: Melting point; ~ 195-200 oC; Sieve residue 63µm; ≤ 0.3%. S content; ≥ 99.5%. |

Use Characteristics		HiDispersion® S-80 is a curing agent for all natural and synthetic rubbers, which require a quick incorporation in the mix and an excellent dispersion of the sulfur. Due to the homogeneous dispersion in the rubber the occurence of localized overcured zones is avoided, which ensures an improved resistance against ageing and dynamic fatigue. The good dispersion of sulfur is of particular advantage in soft compounds, in which a problem-free distribution of the sulfur is often very hard to achieve.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective sulfur is assured.

Dosage levels	Same phr with normal powder sulfur

Applications	Obviously for soft compounds; light-colored compounds, which must be free of sulfur stains,  rubber articles which have to withstand dynamic stress.

Packaging		Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.