LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion®						          Predispersed Rubber Chemicals

TBBS-80     Aaccelerator for the vulcanization of natural and diene synthetic rubbers

Product description

| Composition | 80% dibenzothiazyl disulphide, 20% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | Beige granules |
| Density,20 oC | Approx. ~ 1.17 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of TBBS: Melting point; ~ 106 oC; Evaporation loss; ≤ 0.3 %. TBBS content; ≥ 98%; Sieve residue 63µm; ≤ 0.5 %. Ash content; ≤ 0.3 %. |

Use Characteristics		Delayed action accelerator HiDispersion® TBBS-80 for NR, IR, BR, SBR, NBR, and EPDM. It is suitable used for high temperature kneading and provides a considerably long scorch  time, great processing safety and a fast full cure. HiDispersion® TBBS-80 is used as a independent accelerator for the low sulfur vulcanization or together with  dithiocarbamate or thiuram accelerators. The vulcanizates obtained have good ageing resistance and good moduli. The curing rate of mixes containing HiDispersion® TBBS-80 in combination with thiuram and Dithiocarbamate is noticeably reduced. Thiourea has a strong secondary acceleration effect on HiDispersion® TBBS-80, mainly in mixes containing little sulphur. In compounds which are accelerated with mercaptanes and thiurams, HiDispersion® TBBS-80 may delay scorch.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective TBBS is assured.

Dosage levels	NR:	primary: 0.5 - 1.0 phr with 2.5 - 3.5 phr sulfur

secondary: 0.5 phr with 1.5 - 3.5 phr sulfur and 0.3 phr mercapto or thiuram accelerator;

SBR: 1.0 - 1.4 phr with 1.5 - 2.5 sulfur and 0 - 0.2 phr thiuram accelerator.

Applications	Mechanical articles of all kinds, e.g. treads, carcasses, air hoses, conveyor belts, transmission belts, hoses, cable insulations.

Packing			Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.