LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion®						          Predispersed Rubber Chemicals

TDEC-70  Ultra accelerator for the curing of natural and synthetic rubbers, especially EPDM and IIR

Product description

| Composition | 70 % tellurium diethyldithiocarbamate, 30% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | Orange granules |
| Density,20 oC | Approx. ~ 1.23 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of TDEC: Melting point; ~ 108 oC; Evaporation loss; ≤ 0.5%. TDEC content; ≥ 98%; Sieve residue 63µm; ≤ 0.5 %. Tellurium Content; 16.5 - 19.0 %. Ash content; ≤ 0.3 %. |

Use Characteristics		Super accelerator HiDispersion® TDEC-70 for NR and synthetic rubbers. It causes a high spped vulcanization of EPDM and IIR when used together with other accelerators of the thiazole, thiuram and dithiocarbamate class. Even used in small amounts of HiDispersion® TDEC-70, it gives a shorter total curing time. The vulcanizates using TDEC-70 have high tensile strength, and good aging resistance. Additions of HiDispersion® TDEC-70 are advantageous in soft compounds with a high oil content, since larger dosages of oil reduce the curing rate.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective TDEC is assured.

Dosage levels	HiDispersion® TDEC-70 is used as an additional accelerator together with thiazole, thiuram and dithiocarbamate accelerators. For preventing blooming the dosage should not exceed 0.5 phr.

Applications	It is broadly used in industrial goods, wires and cables, air bags tubes and rubberized clothes; and also used in automobile hoses, steam and acid resistant hoses, profiles.

Packing			Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.