LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion®						          Predispersed Rubber Chemicals

TMTM-80        Ultra accelerator for the curing of natural and synthetic rubbers

Product description

| Composition | 80% tetramethylthiuram mono-sulphide, 20% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | Yellow granules |
| Density,20 oC | Approx. ~ 1.24 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of TMTM: Melting point; ~ 100 oC; Evaporation loss; ≤ 0.5%. TMTM content; ≥ 98%; Sieve residue 63µm; ≤ 0.5 %. Ash content; ≤ 0.5 %. |

Use Characteristics		A super accelerator HiDispersion® TMTM-80 causes very rapid and scorch-safe vulcanization of natural and synthetic rubbers. HiDispersion® TMTM-80 receives additional activation from  basis accelerators, e.g. aldehyde amine and guanidine.

Together with sulphenamide and mercapto accelerators in which HiDispersion® TMTM-80  is used as secondary accelerator are of great technical importance. Low sulphur vulcanization provides vulcanizates with good ageing resistance.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective TMTM is assured.

Dosage levels	NR:	primary: 0.15 - 0.3 phr + 2 - 3 sulfur

secondary: 0.1 - 2.5 phr + 2.5 phr sulfur and 1 phr mercapto accelerator;

SBR:primary: 0.25 - 1.5 phr + 2 - 3.5 phr sulfur

secondary: 0.1 - 0.75 phr + 2 - 3.5 phr sulfur and 2 phr mercapto accelerator;

IIR: primary: 1 - 2 phr + 1 - 2 phr sulfur;

NBR: 0.1 - 3 phr + 0.5 - 2 phr sulfur and 1 - 2 phr mercapto accelerator;

CR: 0.5 - 1 phr + 0.5 - 1 phr sulphur and 1 - 3 phr guanidine accelerator.

Applications	Cable insulations, light color and white vulcanizates, transparent pure rubber articles.

Packaging		Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.