LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion®						          Predispersed Rubber Chemicals

ZBEC-70    Nitrosamine free ultra accelerator for the curing of natural and synthetic rubbers

Product description

| Composition | 70% Zinc-dibenzyl- dithiocarbamate, 30% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | White to grey granules |
| Density,20 oC | Approx. ~ 1.22 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of ZBEC: Melting point; ~ 178 oC; Evaporation loss; ≤ 0.5%. ZBEC content; ≥ 97%; Sieve residue 63µm; ≤ 0.5 %. Zinc Content; 10.0 - 11.5 %; Ash content; ≤ 0.5 %. |

Use Characteristics		A nitrosamine free super accelerator HiDispersion® ZBEC-70 is a fast action thiocarbamate accelerator which has not been found to produce any harmful cancer-causing materials. HiDispersion® ZBEC-70 can be used as a primary or secondary accelerator both in natural and synthetic rubbers, e.g.  EPDM, IR, SBR, NBR, IIR. Compared with conventional dithiocarbamate accelerators, HiDispersion® ZBEC-70 has a high level of processing safety. In compounds containing thiazole or sulphenamide accelerators, HiDispersion® ZBEC-70 has an activating effect. Appropriate matching dosage of Zinc oxide and sulfur when using, the aliphatic acid (e.g. stearic acid) is not necessary. When same molar dosages of ZBEC-70 are used, vulcanizates containing HiDispersion® ZBEC-70 demonstrate similar modulus to other dithiocarbamates.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective ZBEC is assured.

Dosage levels	EPDM:	HiDispersion® ZBEC-70:				0.8-2.5 phr

HiDispersion® S-80:					1.0-2.0 phr

HiDispersion® MBT (MBTS)-80:			1.0-2.0 phr

HiDispersion® CBS-80:					0.5-1.5 phr;

NR, SBR, NBR:	HiDispersion® ZBEC-70:		0.8-2.0 phr

HiDispersion® S-80:					1.0-2.0 phr

HiDispersion® MBT (MBTS)-80:			0.5-3.0 phr.

Applications	Suitable for technical rubber articles based on NR, EPDM, IR, SBR, NBR or IIR. Particularly suitable for light or brightly colored rubber articles.

Packaging		Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.