LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion®						          Predispersed Rubber Chemicals

ZDEC-80      Super accelerator for the curing of natural and diene synthetic rubbers

Product description

| Composition | 80% zinc-diethyl-dithiocarbamate, 20% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | White to greyish granules |
| Density,20 oC | Approx. ~ 1.33 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of ZDEC: Melting point; ~ 174 oC; Evaporation loss; ≤ 0.5%. ZDEC content; ≥ 97%; Sieve residue 63µm; ≤ 0.5 %. Zinc Content; 17.0 - 19.0 %; Zinc Salt Soluble in water; ≤ 0.02 %. Ash content; ≤ 0.5 %. |

Use Characteristics		HiDispersion® ZDEC-80 causes very rapid vulcanization of natural and synthetic rubbers, e.g. SBR, NBR and EPDM. The addition of thiuram and thiazole accelerators can retard the start of the vulcanization and, at the same time, increase processing safety. ZDEC-80 provides a longer scorch time and a faster total curing rate than ZDBC-80. HiDispersion® ZDEC-80 recieves an additional activation from basic accelerators. HiDispersion®ZDEC-80 is also used in small amounts for secondary acceleration and activation of mixes which are going to be cured with mercapto or thiuram accelerators. HiDispersion® ZDEC-80 gives very good tenslie and resilience properties. For improving the resistance to ageing especially of NR and IR it is recommended to add antioxidants.

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective ZDEC is assured.

Dosage levels	NR:	0.3 - 1.0 phr; as secondary accelerator: 0.1 - 0.2 phr;

SBR and NBR:	0.8 - 1.2 phr; as secondary accelerator: 0.1 - 0.2 phr.

Applications	Suitable for technical rubber articles based on NR, EPDM, IR, SBR, NBR or IIR.

Packaging		Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.