LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Accelerators)

HiDispersion®						          Predispersed Rubber Chemicals

ZDMC-80      Super accelerator for the curing of natural and diene synthetic rubbers

Product description

| Composition | 80% Zinc-dimethyl- dithiocarbamate, 20% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | White granules |
| Density,20 oC | Approx. ~ 1.47 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of ZDMC: Melting point; ~ 244 oC; Evaporation loss; ≤ 0.5%. ZDMC content; ≥ 97%; Sieve residue 63µm; ≤ 0.5 %. Zinc Content; 20.5 - 22.0 %. Ash content; ≤ 0.5 %. |

Use Characteristics		HiDispersion® ZDMC-80 causes very rapid vulcanization of natural and synthetic  rubbers, e.g. SBR, NBR and EPDM. The addition of thiuram and thiazole accelerators retards the start of the vulcanization and increases processing safety. HiDispersion® ZDMC-80 gives a longer scorch time and a faster total curing time than ZDBC-80, ZDEC-80 and ZEPC-80. HiDispersion® ZDMC-80 receives an additional activation from basic accelerators. ZDMC-80 is also used in small amounts for secondary acceleration and for the activation of mixes, which are going to be cured with mercapto or thiuram accelerators. HiDispersion® ZDMC-80 provides very good tensile and resilience properties. For improving the resistance to ageing, it is recommended to add antioxidants

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective ZDMC is assured.

Dosage levels	NR:	0.3 – 0.8 phr; as secondary accelerator: 0.05 - 0.3 phr;

SBR and NBR:	0.8 - 1.2 phr; as secondary accelerator: 0.05 - 0.3 phr.

Applications	Suitable for technical rubber articles based on NR, EPDM, IR, SBR, NBR or IIR. Specially for light-colored articles and transparent articles.

Packaging		Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.