LianYungang Lianlian Chemicals Co. Ltd.

Technical Data Sheet (Rubber Additives)

HiDispersion®						          Predispersed Rubber Chemicals

ZnO-80      Curing activator for natural and synthetic rubbers, curing agent for CR rubber.

Product description

| Composition | 80% Finely selected zinc oxide, 20% EPDM/EVA binder and dispersing agents |
| --- | --- |
| Appearance | Milky white granules |
| Density,20 oC | Approx. ~ 2.97 g / cm3 (20oC) |
| Physiological properties : See safety data sheet (MSDS) |  |
| Raw material characteristics of ZnO: Pb%; ≤ 20ppm; Loss on ignition; ≤ 0.1%. ZnO content; ≥ 99.8%; Sieve residue 63µm; ≤ 0.1%. |

Use Characteristics		HiDispersion® ZnO-80 is a special grade of zinc oxide particularly suitable for the  rubber industry. Due to its EPDM elastomer bound form, the absorption of humidity  from the atmosphere during storage is prevented. In comparison to extrusion  compounds containing powdered zinc oxide, those with HiDispersion® ZnO-80 provide smoother profiles. This is due to the more homogeneous dispersion of HiDispersion®  ZnO-80. A slight increase in modulus and tensile strenghth usually occurs; elongation at break is also improved. HiDispersion® ZnO-80 prevents the heat swell which normally occurs when powdered zinc oxide is used in CR mixes

Processing Advantages	The thermoplastic, excellent compatible EPDM/EVA binder which is combined with active dispersing promoters allows much more easily and quickly incorporation and excellent dispersion in the rubber mixing. In this way, optimal activity of the effective ZnO is assured.

Dosage levels	3 - 8 phr

Applications	Curing activator, particulary in the presence of fatty acids for almost kinds of rubbers.

Packaging		Net 25 kg cartons with plastic inner.

Storage stability	In original closed containers under cool and dry conditions max. 2 years.

Handling	Consult material safety data sheet (MSDS) for additional handling information.